## Slide 1: Thermomechanical MMW Spallation Model in ALAMO

## Slide 2
A unified continuum model for millimetre-wave rock drilling
Implementation plan summary — 2026-05-13

## Slide 3: What we are modelling
Millimetre-wave drilling — a high-power microwave beam (~30–300 GHz, kW–MW) heats rock surfaces fast enough that the rock fails before it can melt or vaporise efficiently. Two competing removal mechanisms:
Spallation — thermal stresses crack and detach mm-thick chips.
Vaporisation — surface boils away once enthalpy exceeds latent heat.
The right model has to handle both regimes plus the transition between them.

## Slide 4: Six coupled physics ingredients
Enthalpy heat conduction with solid / liquid / vapour phase tracking.
MMW beam source — Gaussian profile, Beer–Lambert absorption.
Surface losses — radiation + convection.
Voronoi mineral microstructure — per-grain properties, grain boundaries.
Thermoelastic mechanics with damage-degraded stiffness.
Material removal — spall detachment OR vaporisation recession.
All on an adaptive mesh refinement (AMR) grid using the ALAMO framework.

## Slide 5: Why ALAMO
ALAMO is an AMReX-based multi-physics framework with:
A composable integrator pattern (multiple inheritance for coupled physics).
Built-in nodal elasticity operator with multigrid solver.
Voronoi and parser-based initial conditions.
AMR with regrid/average-down already wired up.
We inherit from HeatConduction + Mechanics<…> and add the MMW-specific coupling. No new executable framework — just one new integrator and one new top-level binary, mmwspalling-3d-g++.

## Slide 6: The plan: 18 incremental steps
Each step ends with a verification or validation test with a pass criterion.
Steps 1–4 — Pure thermal physics (no mechanics).
Step 4b — Validation milestone against Zhang/Oglesby MMW heating data.
Steps 5–6d — Heterogeneous microstructure + Hu thermal validation.
Steps 7–7d — Thermoelasticity, AMR, Hu thermoelastic validation.
Steps 8–11b — Damage, cohesive zones, removal, Hu LRST/onset validation.
Steps 12–18 — Revised LEFM Sp + Weibull branch + Kant/Rossi data.

## Slide 7: Validation campaigns
Four independent experimental reference datasets, each anchoring a different piece of the model:
Source | Validates | Status
Zhang & Oglesby (granite MMW heating) | Heat + beam + losses | ✅ done (Step 4b)
Hu (prescribed-T flame heating, granite/sandstone) | Thermal, stress, damage chain | ✅ 6d, 7b/7d, 8b, 11b
Kant 2017 (flame jet, confining pressure) | LEFM onset, pressure dep. | ⏳ Step 12c, 18
Rossi 2018 (post-flame thin-section crack density) | Spall depth profile | ⏳ Step 16

## Slide 8: Where we are today
✅ Completed (Steps 1–11b): full thermo-mechanical-damage pipeline, including Voronoi microstructure, AMR for thermal-stress, Drucker–Prager damage, cohesive zones (unit test), and a working spall + vaporisation removal loop. Three of four validation anchors satisfied.
🔜 Next (Steps 12–18): a runtime toggle adds an alternative LEFM-based spallation block based on a stress-intensity-factor Sp = K_I/K_Ic criterion + per-face Weibull flaw statistics, then closes Kant and Rossi validations.

## Slide 9: Steps 1–4: Thermal foundation
Step | Adds | Verification
1 | Skeleton integrator + build | Runs to t=1
2 | Enthalpy form (solid/liquid/vapour) | Stefan analytic, 4.23% front-position error
3 | Gaussian + Beer–Lambert MMW source | Domain-integrated power, 1.61% error
4 | Surface radiation + convection | Equilibrium temperature, 0.00% error

## Slide 10
Forward-Euler explicit; latent heat handled by closed-form T↔H inversion (no Newton iteration). The Voller–Prakash enthalpy formulation makes phase plateaux exact.

## Slide 11: Step 4b: Zhang/Oglesby validation (mid-plan milestone)
Setup: 10 × 10 × 2.5 cm granite, 28 GHz beam (ω₀ = 2 cm), piecewise-constant power schedule 800 W → 3200 W over 1750 s.
Pass: ALAMO peak surface temperature 2871 K vs. Zhang’s simulation 2850 K at t = 1250 s — 0.7% error (criterion < 15%).
What this exercises end-to-end: enthalpy w/ latent heat, T-dependent material properties (ρ(T), κ(T), c_p(T) polynomial fits), Beer–Lambert absorption with reflectivity, radiation + convection losses, and the implicit backward-Euler thermal solver added during tuning.

## Slide 12: Steps 5–6c: Heterogeneous microstructure
Step 5 — Reproducible seeded Voronoi grains; per-phase {κ, β, E, ρ, c_p, A_D}; is_gb flag at grain boundaries.
Step 6 — Damage-degraded conductivity κ_eff = κ_phase · exp(−α_D D); optional expression-mode microstructure for deterministic laminate tests.
Step 6b — H/T consistency: every phase has its own enthalpy table; the heterogeneous path now advances conserved enthalpy, not temperature.
Step 6c — Grain topology ≠ phase topology. Same-mineral neighbouring grains can now have grain-boundary effects (cohesive zones, elevated A_D).

## Slide 13: Step 6d: Hu prescribed-T thermal validation
First Hu reproduction: flame-jet patch BC on a granite/sandstone cube, mechanics off, heat conduction only.
Hole-1 ΔT range: granite 0 → 35.3 K, sandstone 0 → 73.2 K.
At t = 30 s, L1/L2 line-temperature ratios match Hu within ~3 percentage points (sandstone L1 +15.84% vs Hu +12.58%; L2 +17.38% vs +18.90%).
Establishes the prescribed-T patch BC that all subsequent Hu validations use, ahead of bringing mechanics online.

## Slide 14: Steps 7–7d: Thermoelasticity + AMR
Step 7 — Per-phase (E, μ, β, T_ref) mechanical fields, nodal averaging, full microstructure stiffness rebuild every step.
Step 7b — Hu Granite-2 / Sandstone-2 thermoelastic to 30 s, single level. Peak top von-Mises granite > sandstone, as Hu reports.
Step 7c — AMR regrid repair for discrete fields (phase, grain_id, boundary flags, properties). Linear interpolation of integer phase IDs would smear them; we re-evaluate from physical coordinates instead.
Step 7d — Hu thermoelastic rerun with AMR: ~28× fewer cells than uniform refinement, agreement to 7b within tolerance.

## Slide 15: Steps 8 + 8b: Damage and breakage indicator
Step 8 — Drucker–Prager yield F_DP = √J₂ + α_DP I₁ − k_DP. Continuous damage evolution (RK4, irreversible):
Stiffness degradation E(D) = E (1 − D).
Step 8b — Hu breakage index f_b = σ_v / σ_s, damage evolution off:
Granite f_b = 0.86 (Hu: 0.91), Sandstone 0.84 (Hu: 0.82).
Granite/sandstone margin +16.8% vs Hu +19.7% — correct ordering.

## Slide 16: Step 9: Grain-boundary cohesive zones
Bilinear traction–separation law on true grain-boundary faces (not just phase boundaries):
Linear loading to peak traction f_t at δ_c, linear softening to zero at δ_max.
Calibrated so integrated work = input fracture energy G_c = ½ f_t δ_max.
GB tensile strength set to 40% of intra-grain strength.
Status: unit-test verified (traction–separation curve overlays analytic bilinear law to plotting precision). Traction feedback into the elastic operator deferred — currently a passive diagnostic.

## Slide 17: Steps 10–11: Material removal
Step 10 — Spall detachment. Level-set field φ tracks the surface; columns where D ≥ threshold and σ₁/σ₃ ≥ ξ_s ≈ 8 (Hoek–Brown) detach with thickness h_spall = C_h √(α t_spall). Detached cells reset to ambient.
Step 11 — Vaporisation. Once H ≥ H_vap at a surface cell, advance with RoP_vap = (1−R) P₀ / (ρ L_tot A_beam). Global mode chosen by max(RoP_spall, RoP_vap).
Both modes share fields; per-column decisions use MPI reductions so z-decomposed columns stay coherent across ranks.

## Slide 18: Step 11b: Hu LRST + onset validation
First validation that exercises the full damage pipeline.
 | Granite | Sandstone
ALAMO onset | 37.0 s | 87.0 s
Hu target onset | 31.5 s (±20%) | 76.7 s (±20%)
ALAMO LRST | 776.6 K | 898.7 K
Hu target LRST | 791 K (±10%) | 842 K (±10%)

## Slide 19
✅ All four metrics pass. Granite spalls before sandstone, as observed.
Caveat: sandstone damage zone is deeper than Hu reports (warning-only in v1) and per-rock A_D values are explicit calibration knobs.

## Slide 20: Step 12: The branching point — spallation-model toggle
spallation.model = damage_law (default — Steps 8–11b preserved) spallation.model = sp_weibull (revised LEFM approach — Steps 12–18)
Toggle is a full block swap, not per-component:
Component | damage_law | sp_weibull
Onset criterion | Drucker–Prager | Sp = K_I / K_Ic(T)
Damage evolution | eq.27 RK4 | none (Weibull statistics)
Spall thickness | C_h √(α t_spall) | Sp-vs-depth zero crossing
GB statistics | CZM (Step 9) | Per-face Weibull flaws
Removal granularity | per-column | per-cell

## Slide 21
EOS work (Mie–Grüneisen, linear E(P)) dropped 2026-05-13.

## Slide 22: Why the revised approach?
The damage_law branch works but has two per-rock free parameters (A_D, Ψ₀) tuned to fit Hu. The revised approach replaces both with quantities that can be read from independent literature:
K_Ic(T) from Nasseri 2007 piecewise-linear table (5 measured points).
Weibull (a₀, m) from Westerly granite microcrack statistics.
The goal is predictive, not fitted: same parameters work across Hu, Kant, and Rossi without per-test recalibration.

## Slide 23: Steps 12–13: Sp criterion + AMR refinement
Step 12 — Sp onset. Tada weight function
with f_K(ξ) = (1.3 − 0.3 ξ^{5/4})/√(1−ξ²) and Simpson quadrature with logarithmic refinement near the crack tip.
Verification: Kant 2017 closed-form Bi < 0.5 regime, ALAMO Sp(t) matches analytic Sp_red within 5% over the first 10 s.
Step 13 — Production AMR refinement criteria (|∇H|, |∇D| or |∇Sp|, beam footprint) + adaptive Δt per CFL bound.

## Slide 24: Steps 15–17: Weibull, depth, per-cell removal
Step 15 — Per-face flaw lengths sampled at init: GB faces a_f ~ Weibull(a₀_gb, m), intragranular a_f ~ Weibull(a₀_ig, m) with a₀_ig ≈ a₀_gb / 5 (Rossi 2018). Re-runs Hu LRST/onset without per-rock fitting.
Step 16 — h_spall(x,y) = max{ z : K_I(x,y,z;a) ≥ K_Ic(T(x,y,z)) } evaluated by re-running the Tada integral down a column. Validated against Rossi 2018 crack density vs depth (peak at 100–200 µm).
Step 17 — Per-cell normal velocity v_n(x,y,t): spall and vaporisation can fire at different (x,y) within the same beam footprint in the same step. Re-runs Zhang/Oglesby.

## Slide 25: Step 18: Confining-pressure validation (Kant 2017)
Lithostatic pressure applied as a stress-field BC on side faces — not through a Ψ₀(P_c) empirical correction. Pressure enters the LEFM criterion implicitly through σ_xx.
Pass criteria: - Onset ΔT at p = 0 inside Kant’s measured 553–694 °C bracket. - Monotone-decreasing onset ΔT across p ∈ {0, 27, 48} MPa. - Slope vs pressure within ±30% of Kant’s measured trend.

## Slide 26: Step 14: End-to-end Hu reproduction (both branches)
Runs twice, once per branch, on the same Hu setup:
Under damage_law: consolidates 6d → 7b/7d → 8b → 11b.
Under sp_weibull: consolidates 6d → 7b/7d → 12c → 15a — must reproduce Hu LRST/onset without the per-rock fitting that 11b relies on.
This is the final non-MMW spallation validation. Two passing branches give us an apples-to-apples comparison of the empirical and LEFM approaches on the same data.

## Slide 27: Open caveats and deferred work
Cohesive-zone traction feedback into the elastic operator (Step 9).
AMR moving-surface validation with spall/vap removal (Steps 10–11).
Sandstone damage depth in Step 11b is larger than Hu — warning only.
Implicit thermal solver is single-level + Neumann BCs; not yet compatible with fracture mechanics.
Mie–Grüneisen / linear E(P) dropped 2026-05-13 — no pressure-dependent stiffness in either branch.
Step 11b damage parameters (A_D) are fitted, not predictive — Step 15 is the answer.

## Slide 28: Summary
11 of 18 steps complete, including three of four validation anchors (Zhang/Oglesby, Hu thermal/thermoelastic, Hu LRST/onset).
The model is a faithful re-implementation of the unified MMW drilling theory from main.tex, on top of ALAMO’s AMR multi-physics infrastructure.
The remaining Sp + Weibull branch (Steps 12–18) replaces fitted damage parameters with literature-anchored LEFM + flaw statistics, validated against Kant 2017 and Rossi 2018 alongside the existing Hu data.
The two-branch toggle lets us compare the empirical and LEFM formulations head-to-head on identical setups.